WEEK 5 – SPL 5

Pure metals – ductile and soft

This softness arises because of their low lattice resistance — that is, there are few obstacles in the crystal structure to resist dislocation motion (which leads to plastic deformation).

Therefore, to make the ‘stronger’ we use:

| Method | Mechanism | Process | Microstructure Effect | Typical Application |
| --- | --- | --- | --- | --- |
| Solid Solution Strengthening | Solute atoms distort the crystal lattice, hindering dislocation motion | Add alloying elements; atoms dissolve into solid solution (e.g., Zn in Cu) | Uniform solid solution, lattice strain due to atom size mismatch | Brass (Cu-Zn), Stainless steel (Cr in Fe) |
| Precipitation Hardening | Fine precipitates form and obstruct dislocations | Heat treat to form solid solution, quench, then age to form precipitates | Precipitates dispersed in the matrix (e.g., CuAl₂ in Duralumin) | Al-Cu (Duralumin), Ni-based superalloys |
| Work Hardening | Plastic deformation increases dislocation density, which entangles | Cold working (e.g., rolling, drawing, hammering) | High dislocation density and strain-hardened regions | Cold-rolled steel, metal forming processes |

Solid solution – substitutional (big) and interstitial (small)

METAL TYPES

FERROURS ALLOYS – IRON IS THE PRIME CONSTITUENT- low carbon steel, high carbon steel, stainless steel, cast iron, grey iron and white iron.

NON- FERROUS ALLOYS – copper alloys, aluminium alloys, titanium alloys and magnesium alloys.

TAXONOMY OF METALS

Anything below 1.4% carbon = steels- can plastically deform

Anything above = cast iron

Types of cast iron

1. Gray Cast Iron

- Graphite in flakes (sharp, irregular shapes)

- Flakes act as stress concentrators → weak under tension

- But it's stronger under compression and offers:

  - Excellent vibration damping (used in machinery bases)

  - Good wear resistance

- Matrix = ferrite (softer) or pearlite (stronger)

2. Ductile (Nodular) Iron

- Made by adding Mg or Ce → changes graphite to nodules (spheres)

- Spheroidal graphite means less stress concentration → much better ductility and toughness

- Matrix is often pearlitic for strength

3. White Cast Iron

- No graphite; carbon is mostly iron carbide (Fe₃C or cementite)

- Very hard and wear-resistant, but very brittle

- Formed via fast cooling, doesn't allow graphite to form

4. Malleable Cast Iron

- Made by heat treating white iron at 800–900°C for 30+ hours

- This transforms iron carbide into graphite "rosettes"

- Offers good ductility with moderate strength

NON- FERROUS

Nonferrous alloys are metallic alloys that do not contain iron (Fe) as a major component. These materials are often valued for:

- Lightweight

- Corrosion resistance

- High strength-to-weight ratio

- Specialized thermal or electrical properties

Cost depends on melting as all materials need to be melted to be processed

DESIGN CONSIDERATION

| Design Challenge | Explanation |
| --- | --- |
| Cooling Shrinkage | Metals contract when cooled from melt, which affects dimensional accuracy. |
| Air Gap Formation | Shrinkage during cooling creates a gap between metal and mould, reducing heat transfer. |
| Work Hardening | Plastic deformation increases strength, limiting further shaping unless annealed. |
| Limited Plastic-Forming | Excessive deformation risks cracking; shaping must be done in steps. |
| Corners Difficult to Form | Metals struggle to fill sharp mould corners, leading to defects. |
| Unidirectional Pressing | Forging presses push in one direction; liquids can fill complex moulds better. |
| Phase Changes | Structural changes on heating/cooling influence mechanical properties and process control. |

INGOT CASTING- usually reheated/reshaped into useful products – is the first stage

- Ingot casting involves pouring molten metal into molds to form simple, solid shapes called ingots.

- The melting temperature of a material determines the casting process and mold design.

- Metals must be heated above this temperature to be cast, and mold materials must withstand it without degrading.

Q: What are typical mold characteristics for ingot casting?
A: Molds are generally simple in shape with rounded corners. This design eases removal of the solidified ingot and minimizes stress concentrations that might lead to cracks during cooling.

Q: What is meant by the grain structure in metals?
A: After solidification, metals develop a crystalline grain structure. The nature of this structure affects mechanical properties like strength and toughness.

Q: What causes the contraction cavity at the top of the ingot?
A: As molten metal cools, it shrinks. Since solidification starts at the mold walls and proceeds inward and upward, a cavity often forms at the top, where the last part remains molten and contracts as it solidifies.

Q: What happens to impurities during solidification?
A: Impurities are usually expelled from the solidifying front and concentrated in the last melt zones, which often end up at the top of the ingot.

Q: How do gas bubbles form during ingot casting?
A: Gases (like nitrogen) that were dissolved in the molten metal can come out of solution upon cooling, forming gas bubbles or porosity in the ingot.

PROBLEMS WITH INGOT CASTING

- Contraction cavities

  - Ingot casting creates a shrinkage hole at the top because metal shrinks when it cools.

- Segregation of impurities

  - Impurities (and alloying elements) are pushed to the last melt zones, usually the center or top, creating non-uniform composition.

- Gas porosity

  - Gases like nitrogen can get trapped and form bubbles or voids.

- Larger starting size

  - Ingots are large, so more energy and effort is needed to shape them later (e.g., into sheets or rods).

Therefore, CONTINUOUS CASTING

- No shrinkage cavity

- Less segregation:

- The columnar grains (crystals) form over shorter distances, so impurities don't have time to separate much — leading to more uniform material.

- Smaller product = less work later:

- The output is already in slab or rod shape, so less rolling or forging is needed later to get it into usable form.

Continuous Casting:

- Uses a permanent mould (like a water-cooled copper mould).

- The molten metal flows continuously, solidifies, and exits as a solid bar or sheet.

- There is no expendable pattern or mould — it is reused over and over.

- Used for producing slabs, billets, and blooms (like in steel mills).

PERMANENT PATTERN (SAND CASTING)

Sand casting is a method where molten metal is poured into a mold made of sand. Once the metal cools and solidifies, the sand mold is broken to remove the final part.

- A pattern is made (usually wood, metal, or plastic).

- It is pressed into sand to make a mold cavity.

- The pattern is removed, leaving behind the shape.

- A core may be added for internal features.

- Molten metal is poured into the mold via the gate.

- Once it cools and solidifies, the sand is broken apart, and the casting is removed.

- The mold is discarded, but the pattern is reused to make more castings.

Why use this method?

- Low cost for small production runs

- Flexible shapes (including complex geometries)

- Large parts can be made easily

- Reusable pattern makes it cost-effective over many castings

Automated sandcasting

Automated sand casting uses machines to rapidly and repeatedly form sand molds, enabling high-volume production of cast parts. This method dramatically increases casting speed compared to traditional hand-packed molds.

DIE CASTING / PERMANENT MOULDS

Die casting involves injecting molten metal under pressure into a reusable metal mould (die) to produce accurately shaped parts. Unlike sand casting, the mould is not destroyed after each use — it’s opened and reused for thousands of cycles.

High-temperature materials needed for the die:

- Since molten metal is hot, the die must be made of materials like hardened tool steel that can withstand repeated heating.

Limits the process to lower melting point metals:

- Dies cannot handle extremely high temperatures (like for steel), so this process is mostly used with aluminium, zinc, magnesium, etc.

High cost of moulds (dies):

- Dies are expensive to manufacture due to the complex design, precision machining, and materials.

- This is why die casting is economical only when:

  - Producing large quantities (to spread the mould cost),

  - Making small components (less metal = less heat = longer die life).

Expendable Mould (Investment Casting)

- Making a wax model of the part

- Coating it in ceramic to form a mould

- Melting away the wax (hence “lost wax”)

- Pouring molten metal into the hollow ceramic shell

- Breaking the shell to reveal the final part

FORMING – METAL FABRICATION METHODS

| Process | Force Type | Product Type | Notes |
| --- | --- | --- | --- |
| Forging | Compressive | Tools, shafts | High strength; hot or cold |
| Drawing | Tensile | Wires, tubes | Requires clean, lubricated dies |
| Rolling | Compressive | Sheets, rails, beams | Hot = easy forming, Cold = better finish |
| Extrusion | Compressive/Ram | Long rods, hollow tubes | Ductile metals, continuous profile |

FORGING Method: A metal blank is placed between dies and hit with a hammer or press.

DRAWING Method: A metal rod is pulled through a die, reducing its cross-sectional area.

ROLLING Method: A metal piece is passed between two rotating rolls.

EXTRUSION Method:

- A metal billet is placed in a chamber.

- A ram pushes it through a die.

- The metal flows out as a continuous profile.

METAL FORMING

We use metal forming because casting has defects – cant fill voids/ cavity and holes therefore cost can be reduced FORMING BETTER IMPROVED MECH PROPERTIES

Long shapes harder to cast

Best casting from EUTECTIC ALLOYS but not always desirable

INHOMOGENITY- common in casting but plastic deformation reduces this. Casting often causes uneven structure due to cooling. Forming evens it out through plastic deformation.

Some materials difficult to process as liquid due to high MELT temp – REFRACTORY MATERIALS -  better shaped through forming or powder processes.

CLASSIFICATIONS OF FORMING PROCESSES

FORGING

Hot Forging

- Benefits:

  - Allows large deformations (big changes in shape)

  - Easier to shape metals due to reduced strength at high temperatures

- Drawbacks:

  - Poorer surface quality

  - Lower dimensional accuracy

  - Problems like oxidation (metal reacting with air) and warpage (distortion when cooling)

Cold Forging

- Benefits:

  - Produces more precise parts

  - Results in a better surface finish

- Drawbacks:

  - Requires higher pressures to deform metal (since it's not softened by heat)

  - Limited deformation due to work hardening (material becomes stronger and harder as it's shaped)

| Process | Cold or Hot? | Reason |
| --- | --- | --- |
| Drawing | ✅ Cold forming | Performed at room temperature |
| Hot forging | ❌ Hot forming | Involves heating metal above recrystallization temp |
| Sand casting | ❌ Not a forming process | It's a casting process |
| Welding | ❌ Joining process | Not forming at all |

- Formability and Bend Radius

- Formability is how easily a sheet can be bent or stretched without cracking.

- It's often measured as the minimum bend radius in multiples of sheet thickness (t):

  - t = 1 → excellent (can bend sharply)

  - t = 4 → average (needs wider bend)

2. Radii Design Rule

- Bending edges and corners should have large radii.

- Ideally, radius ≥ sheet thickness to prevent cracking during bending.

3. Stretching & Drawing Limits

- Formability also affects how far a sheet can be stretched or deep drawn (e.g. into a cup shape).

- Poor formability leads to necking (local thinning) and failure.

4. Forming Limit Diagrams (FLDs)

- FLDs provide a quantitative guide to forming safety.

- They plot strain combinations (major vs. minor strain) that a sheet can survive before failing.

- Used in advanced simulations and product design to predict failure points.

5. Design Strategy

- Engineers design components to ensure strain levels stay below the forming limit, as shown in FLDs.

- This prevents tearing, cracks, or part rejection during manufacturing.

| Feature | Hot Rolling | Cold Rolling |
| --- | --- | --- |
| Temperature | High (T > 0.35 Tₘ) | Low (T < 0.35 Tₘ) |
| Pressure | Low | High |
| Surface Finish | Rough | Smooth |
| Strength | Low | Higher (due to work hardening) |
| Accuracy | Less | More |

Rolling

Well designed rolling mills have rolls of small diameter (primary roller) these can be supported by additional secondary roles which do not touch the work piece!!

FORGING OF A GEAR CHECK HAND NOTES

METAL CONSIDERATIONS

📉 Left: Idealized (Perfectly Plastic) Material

📈 Right: Real Metal Behavior (with Work Hardening)

- Stress increases again after yielding due to work hardening.

- As the metal is deformed, it becomes stronger and harder, resisting further deformation.

Real metals are not perfectly plastic

- They exhibit work hardening (also called strain hardening), which limits how much they can be deformed.

Work hardening increases hardness

- This can be useful for strength, but also makes further shaping harder.

Cold working vs. Hot working

- This difference in behavior underpins the contrast:

  - Cold working happens below recrystallization → strong but difficult to deform

  - Hot working allows easier shaping with less hardening

Cold worked metal = Stiff, hard, strong AND Higher forces are needed to deform hardened metal

SHEET DEFORMATION

| Process | Description | Key Stress State | Notes |
| --- | --- | --- | --- |
| Blanking | Cutting sheet using punch & die | Shear | Removes a shape from the sheet |
| Deep Drawing | Forming sheet into a cup or can | Biaxial/Triaxial | Involves bending and stretching |
| Limitation | Side walls may fracture | Tensile stress | Walls thicken; overstretching causes failure |

Deep Drawing:

- No volume change:
The material doesn't lose volume, so side walls may thicken as the material is drawn inward.

- Stress conditions:

  - Most of the process involves biaxial stresses (stretching in two directions).

  - Some regions (like the flange) experience triaxial stress (important in fracture behavior).

- Deformation Limits:

  - Limited by the ability of the side walls to carry the tensile loads.

  - Eventually, if overstretched, the walls fracture or tear.

HOT WORKING

Hot worked metals can exhibit 2 features:

- REDUCED YIELD STRESS

- RECOVERY AND RECRYSTALLISATION

MACHINING

Machining refers to processes where material is removed (cut, ground, or milled) from a workpiece to shape it with high precision. Examples include:

- Turning, milling, drilling, grinding, and CNC machining

Often a secondary operation to ‘finish’ parts produced by e.g., casting.

Sometimes it is PRIMARY process:

- Low-volume production

- Prototyping

Doesn’t need dedicated tooling for each part — generic machines like CNC mills or lathes can handle various designs.

Tooling costs = LOW!

CUTTING PROCESSES

JOINING – METAL FABRICATION METHODS

🔥 Brazing

- Uses heat and a filler metal (like solder) to join parts without melting the base metal.

- Gas torch shown adding filler between closely fit metal pieces.

- Moderate strength, commonly used in pipes and electronics.

🔄 Friction Welding

- Parts are rotated and pressed together.

- Friction heats the interface, and pressure bonds them without melting.

- Often used in automotive/aerospace shafts.

🔊 Ultrasonic Welding

- A vibrating tool (sonotrode) applies high-frequency mechanical vibrations with pressure.

- Used for plastics or light metals (e.g., copper wires, lithium-ion batteries).

- Fast, clean, and no filler needed.

🔩 Bolting

- Mechanical fastener (bolt + nut or threaded hole).

- Easy to assemble/disassemble.

- Common in construction, automotive, machinery.

| Phase | Properties | Use in steel |
| --- | --- | --- |
| Pearlite | Strong but softer than martensite | Ductile & used in mild steels |
| Martensite | Extremely hard & brittle | ✅ Main strengthening phase |
| Bainite | Harder than pearlite, softer than martensite | Good compromise phase |
| Austenite | Only stable at high temperature | Not strong, used before quenching |

links with annealing pic!  Refine grain size!

- Makes very soft steel therefore increase ductility. DUCTILITY = able to bend and stretch without breaking A ductile material can undergo a lot of plastic deformation before it fractures.

- Think of it like this: You can bend, stretch, or draw it into a wire without it snapping.

Steel Heat Treatment Phases — Simple Explainer

🟣 1. Austenite (γ)

- When? At high temperature (~800°C)

- What is it? A solid solution of carbon in face-centered cubic (FCC) iron.

- Important because? It’s the parent phase. All other phases come from it depending on how you cool it.

🟡 2. Pearlite

- When? Forms if you cool slowly

- How? Carbon atoms have time to diffuse out, forming alternating layers (lamellae) of:

  - Ferrite (soft) + Cementite (hard)

- Properties: Strong and ductile, but not very hard

- Seen in: Normal air-cooled steel

🔵 3. Martensite

- When? Forms if you quench (rapidly cool)

- How? Cooling is so fast that carbon can’t diffuse, so atoms are “trapped”

- What happens?

  - The crystal distorts into a Body-Centered Tetragonal (BCT) shape

- Properties: Very hard and brittle

- Key fact: It is a diffusionless and very rapid transformation

- Seen in: Tool steels, hardened blades

🟢 4. Tempered Martensite

- When? You take martensite and reheat it slightly

- Why? To reduce brittleness and improve toughness

- Used in: Spring steels, knives, structural parts

| Cooling Rate | Phase Formed | Process | Properties |
| --- | --- | --- | --- |
| Slow (air) | Pearlite | Annealing | Strong, ductile |
| Medium (oil) | Bainite | Normalizing | Moderate strength/toughness |
| Rapid (water) | Martensite | Quenching | Very hard, brittle |
| Martensite + heat | Tempered Martensite | Tempering | Tough + hard (good balance) |

Summary Table: Metal Processing Techniques

| Technique | Type | Key Features / Purpose | Notes / Examples |
| --- | --- | --- | --- |
| Sand Casting | Casting | Uses expendable sand moulds | Good for large parts, low cost, rough finish |
| Die Casting | Casting | Uses reusable metal moulds | High precision, for low-melting alloys |
| Investment Casting | Casting | Expendable wax pattern and ceramic shell | High accuracy, complex shapes |
| Continuous Casting | Casting | Solidifies metal into sheet/bar directly | Used in steel industry, avoids contraction defects |
| Forging | Forming | Deforms metal using compressive force | Improves grain flow, strong parts |
| Drawing | Cold Forming | Pulls metal through die to reduce size | Used for wires, tubing |
| Rolling | Forming | Compresses metal between rollers | Hot or cold, makes sheets and I-beams |
| Extrusion | Forming | Forces metal through die | Rod/tube shapes; hot or cold |
| Machining | Secondary / Primary | Cuts metal to shape with tools | CNC, milling, drilling; good finish |
| Powder Metallurgy | Forming | Compacts metal powders and sinters | For high-melting metals like tungsten |
| Brazing | Joining | Fills joint with molten filler metal | No melting of base parts |
| Welding | Joining | Fuses parts by melting | Strong joint, not removable |
| Bolting/Fastening | Joining | Mechanical attachment | Removable, uses screws/bolts |
| Annealing | Heat Treatment | Heat then slow cool | Softens metal, refines grains |
| Quenching | Heat Treatment | Rapid cooling from high temp | Forms hard martensite |
| Tempering | Heat Treatment | Reheats quenched steel slightly | Reduces brittleness of martensite |
| Normalizing | Heat Treatment | Air cool from above critical temp | Refines grain structure |
| Spheroidizing | Heat Treatment | Hold just below critical temp | Increases ductility for machining |

SPL 6 – CERAMICS

Ceramics are: = non-metallic compounds made from metal + non-metal elements.

- Inorganic & non-metallic materials.

INORGANIC - made from natural elements like silicon, oxygen, aluminum - Not made of carbon chains (unlike organic materials like plastics or wood)

- Made from metal + non-metal elements.

- Bonding is ionic or ionic with some covalent.

- Name comes from Greek "keramikos" (pottery, "to burn").

Traditional Ceramics:

- Used before 1950, made mainly from clay.

- Includes china, porcelain, bricks, tiles, glass.

- After 1950: new materials and better understanding → advanced ceramics.

- Now "ceramic" = a broad category of materials.

European Ceramics Production (2005–2011)

- 📉 Production peaked in 2007 (~35 billion euros), then dropped sharply around 2009 — likely due to the global financial crisis.

- 🧱 Wall & floor tiles and bricks/roof tiles dominate the market.

- 🔬 Technical ceramics and abrasives make up a smaller portion.

- 📈 Recovery starts after 2009 but doesn’t reach pre-crisis levels by 2011.

Modern Technical Ceramics

Recent Materials Advances: Improvements in ceramic materials have made them essential in modern engineering due to their enhanced properties.

Wear and Corrosion Resistance: Ceramics are highly resistant to wear and corrosion, making them ideal for harsh environments such as in pumps, nozzles, and valve parts where durability is critical.

Thermal Properties: Ceramics can withstand high temperatures and resist thermal shock (sudden temperature changes), which is valuable for automotive engine components where materials must endure intense heat and rapid cooling.

Precision Manufacturing: Modern techniques allow ceramic parts to be made with extreme precision, with tolerances within a fraction of a micron. This makes them suitable for high-tech and delicate applications like electronics and aerospace.

Ceramic Material Groups

1.Structural Ceramics -used in high temp applications

- Used where strength + heat resistance are needed.

- Examples: engine parts, cutting tools, furnace linings.

- Materials:

  - Si₃N₄ (silicon nitride)

  - Al₂O₃ (alumina)

  - ZrO₂ (zirconia) — tough and strong at high temps.

2. Electrical Ceramics

- Used in electronics and magnets.

- They can conduct or store electricity in special ways.

KEY APPLICATIONS:

- Capacitors – to store electrical charge

- Sensors – especially in medical or ultrasonic devices

- Piezoelectric components – generate voltage when squeezed (used in microphones, ultrasound, ignition systems)

- Examples:

  - PZT (used in sensors & ultrasound)

  - BaTiO₃ (a capacitor material)

3.Bioceramics

- Used in the human body — safe and non-reactive.

- Examples:

  - Al₂O₃ for hip joints

  - Hydroxyapatite mimics bone

  - Glass used in dental and bone repair

Seals and industrial machine parts

Why ceramics are used here:

- Applications need:

  - Wear resistance (must not degrade easily with use)

  - High surface finish (smooth, precise surfaces)

  - Low friction (so parts move easily without damage)

  - VERY HIGH TEMP THESE MATERIALS NEED TO HAVE HIGH STRENGTH !

Ceramics used:

- Alumina (Al₂O₃) – common, strong, corrosion-resistant

- Silicon Carbide (SiC) – extremely hard, good at resisting wear

- Silicon Nitride (Si₃N₄) – strong, tough, and handles shocks

Key ceramic properties:

- Hardness – resists scratches and deformation

- Low porosity – fewer tiny holes means stronger and smoother

- Machinability to high finish – they can be shaped and polished very precisely

- Corrosion and wear resistance – perfect for harsh machine environments

TURBINE STATOR

A turbine stator is a stationary part of a turbine (like in a jet engine or power plant - It directs high-speed hot gas onto the rotating blades

Application Requirements:

Turbine stators face extreme environments, so the materials must handle:

- Thermal shock resistance: sudden temperature changes without cracking

- Oxidation resistance: avoid reacting with air at high temperatures

- High-temp stability: maintain shape and strength when very hot

- Complex aerodynamic shape: must be precision-shaped to guide airflow

Candidate Ceramics:

- Si₃N₄ (Silicon Nitride)

- SiC (Silicon Carbide)
→ These are advanced ceramics known for high heat and wear resistance.

Key Properties:

- High strength: withstands stress and load

- Moderate to low thermal expansion: resists size change when hot (important for tight fits)

- Good thermal conductivity: can manage heat without overheating

- Fabricatable into complex shapes: essential for aerodynamic designs

HEATING ELEMENT

Requirements of the application:

- Must generate heat when electricity flows.

- Needs to survive high temperature and repeated thermal cycling (heating and cooling again and again).

Candidate Ceramics:

MoSi₂ (Molybdenum disilicide) SiC (Silicon carbide) C (Carbon), ZrO₂ (Zirconia) – doped to modify its electrical/thermal behavior.

Key Properties:

- Needs semiconductor-like resistivity:
➤ Not a perfect conductor (like copper),
➤ Not a perfect insulator either.
➤ This balance lets it generate heat efficiently.

- Also must resist oxidation and remain stable in furnace conditions.

Why Semiconductor?

- Semiconductors allow controlled resistance:
 Higher resistance → More heat (Joule heating)
 But low enough to still let current flow.

- Metals would overheat or oxidize too quickly.

- Semiconducting ceramics handle extreme temps without breaking down.

HEAT SINK FOR TRANSISTOR DEVICES

A heat sink is a component used to pull heat away from electronic parts like transistors so they don't overheat.

A transistor is a tiny electronic component that acts like a switch or an amplifier for electrical signals.

| Aspect | Details |
| --- | --- |
| Purpose | Dissipate heat from transistor devices (e.g., Si, GaAs chips) |
| Application Needs | - Rapid heat dissipation- Low electrical loss- Compatibility with chips |
| Candidate Ceramics | - BeO (Beryllium Oxide)- AlN (Aluminium Nitride)- Diamond |
| Key Properties | - High thermal conductivity (fast heat transfer)- High electrical resistance (electrical insulation)- Low dielectric constant (suitable for high-frequency circuits) |
| Where found in | Computers & laptops – especially CPUs and GPUs |

FURNACE INSULATION

| Category | Details |
| --- | --- |
| Requirements of the application | Withstand high temperatures, retain heat within furnace |
| Candidate ceramics | Porous fire bricks, fiberboard, 'wool' insulate furnace |
| Key properties | Low thermal conductivity, high-temperature stability |

MINIATURE CAPACITOR

A miniature capacitor is a small electrical component used to store and release electrical energy in electronic circuits.

Think of it like a tiny battery, but it charges and discharges very quickly

- High dielectric constant → more charge stored in a small size

- Good temperature stability

- Low loss → efficient performance

| Aspect | Details |
| --- | --- |
| Application Requirement | High charge-storage capability |
| Candidate Ceramics | Various titanates and mixed zirconate-titanates |
| Key Properties | High polarizability, high dielectric constant, low dielectric loss |

| Feature | Purpose/Benefit |
| --- | --- |
| High charge storage | Needed for compact, powerful electronics |
| Titanate ceramics | Good electrical properties for capacitor function |
| High polarizability | Enhances electric field interaction |
| High dielectric constant | Allows more charge storage in small volume |
| Low dielectric loss | Keeps energy loss and heat generation minimal |

HIGH SPEED, HIGH LOAD BEARING

A high-speed, high-load bearing is a mechanical component that:

- Supports rotating or moving parts (like a shaft or wheel)

- Withstands very heavy loads

- Operates at high speeds without failing

APPLICATION REQUIREMENTS:

- High contact loads: Must withstand heavy pressure.

- Wear resistance: Should not degrade quickly.

- Low friction: Important for speed and efficiency.

- Heat dissipation: Must release heat fast to avoid damage.

| Category | Details |
| --- | --- |
| Application Requirements | - Resistance to high contact loads- Wear resistance- Low friction- Heat dissipation |
| Candidate Ceramics | - Silicon Nitride (Si₃N₄) |
| Key Properties | - High toughness and strength (resists breakage under load)- High hardness (resistant to wear)- Very low porosity (fewer internal flaws, better reliability)- Machinable to high surface finish (smooth = less friction)- Moderate to high thermal conductivity (helps carry away heat during use) |
| Use Case Summary | Ideal for extreme mechanical and thermal environments like aircraft engines, racing cars, and precision machines. Combines strength, precision, and durability. |

TRANSDUCER

A transducer is a device that converts one form of energy into another. In this case, it converts mechanical movement (displacement or pressure) into an electrical signal.

| Element | Explanation |
| --- | --- |
| Requirements | Detect tiny movements (like pressure or vibration) and turn them into voltage. |
| Candidate Ceramic | PZT (Lead Zirconate Titanate) – a piezoelectric ceramic. |
| Working principle | When PZT is squashed or stretched, it generates voltage – just like how old weighing scales used to work. |
| Diagram (right) check ppt | Shows a block of PZT. When pressed (force applied), the gauge detects electricity produced from the deformation. |

CUTTING TOOLS

● Requirements of the applications:
Ceramic grades run at high speeds and feeds on a variety of work piece materials.
Typical ceramic applications include turning, grooving, and machining of tough materials like hardened steels.

● Candidate ceramics:
ZrO₂ (Zirconia), WC (Tungsten Carbide)

● Key properties:
Zirconia ceramic has the highest strength and toughness at room temperature of all engineering ceramics.

- High hardness (for cutting tough materials)

- High toughness (resists cracking or breaking)

- Good thermal stability (can handle heat from friction)

Drill bit – used in hand drills or machines to make holes in metal or wood.

Other examples: Lathe tool insert, End mill cutter AND Ceramic scissors (like shown in the slide)

| Property | Why It's Useful in Cutting Tools |
| --- | --- |
| High strength | Allows the tool to resist breaking under pressure. |
| Toughness | Withstands shock loads without cracking. |
| Hardness | Helps cut even tough materials like steel. |

GRINDING MILL PARTS

Requirements of the applications:
Grinding mills are used to crush and grind solid materials into smaller particles. These machines require components that can withstand very high wear and friction.
That’s why ceramics are used for parts like:

- Liners (interior walls)

- Agitator screws

- Rollers

● Ball mill balls:
The balls inside a ball mill (a type of grinder) are made from the same ceramic material as what’s being ground. This avoids contamination.

What’s a mill?
A mill is a machine that breaks down solids into finer particles.

- Grinding mill = breaks/crushes things

- Ball mill = filled with ceramic/metal balls that tumble and crush material

NOZZLES

| Aspect | Details |
| --- | --- |
| Application Requirements | - Chemical and wear resistance (scrubber nozzles) - Withstand high-speed fluid flow (cleaning nozzles) thus wear resistance is essential - CERAMICS High heat resistance used in- (welding/burner nozzles) |
| Reason Ceramics Are Used | - Ceramics provide excellent wear and chemical resistance - Handle abrasive and hot conditions without degrading |
| Examples of Use | - Scrubber systems in chemical plants - High-pressure water jets - Welding/burner nozzles (extreme heat) |

MEDICAL EQUIPEMENT AND CHEMICAL ANALYSER PARTS

- The chemical stability of ceramics permits their application to the artificial kidney pump.

- Free from corrosion and superior in cleaning properties, ceramic materials are also used in blood valves.

| Aspect | Details |
| --- | --- |
| Application | Artificial kidney pumps, blood valves, chemical analyser parts |
| Reason ceramics are used | - Chemically stable (won’t degrade in harsh environments) - Corrosion-resistant - Easy to clean (important for medical hygiene) |
| Key benefit | Safe for internal medical devices due to bio-inertness and cleanliness |

FOOD PROCESSING MACHINNE PARTS

| Aspect | Details |
| --- | --- |
| Application | Food processing machines – kneading rollers, valves, pumps |
| Reason ceramics are used | Ceramics are inherently clean and easy to sterilize |
| Key Benefit | Simplifies hygiene and cleaning procedures – essential in food industry |

- Ceramics don’t corrode or react with food ingredients, which makes them safe and durable for repeated food contact.

- Their smooth surface reduces bacterial buildup.

ISUZU ENGINE

An Isuzu engine is an internal combustion engine made by Isuzu Motors, a Japanese company GAS TURBINE!!

| Aspect | Details |
| --- | --- |
| Application | Engine components (e.g. gas turbines, glow plugs) |
| Why ceramics are used | Excellent thermal efficiency, low energy loss, and heat resistance use of ceramic glow plug - Traditional ones are metal, but ceramic glow plugs heat up faster, reach higher temperatures, and are more durable—this improves engine efficiency and reduces emissions. |
| Key benefits | Clean energy consumption, withstands high temperatures, durable in engine environments |

CERAMIC PROCESSING

| Step | Explanation |
| --- | --- |
| 1. Milling | Raw ceramic powders are mixed in distilled water and ground to reduce particle size. |
| 2. Drying & Granulation | Water is removed; the powder is crushed and sieved to break agglomerates. |
| 3. Compaction | The dried powder is placed in a die and pressed into shape (e.g., block, disc). |
| 4. Sintering | The compacted part is heated in a furnace just below melting point. This bonds particles together and densifies the material. |

Milling

- What it means: Breaking down raw ceramic materials into very fine powder.

- Why it's done: To reduce particle size and ensure uniformity for shaping and sintering.

🔹 Agglomerated

- What it means: When fine powder particles stick together into clumps or clusters.

- Why it matters: These clumps must be broken (by granulation) to ensure even shaping and prevent defects.

🔹 Sintering

- What it means: Heating the pressed powder (but not melting it!) to bond the particles together.

- Why it's important: It densifies the material, increases strength, and gives it final properties.

🔹 Green Part

- What it means: The shaped ceramic component before sintering.

- Think of it as: A fragile, chalk-like version of the part that hasn’t been fired yet.

- Fun fact: It’s called "green" not because of color, but because it’s not “finished” or fully processed yet.

CERAMIC INJECTION MOULDING

| Step | Explanation |
| --- | --- |
| 1. Mixing | Fine ceramic powder is combined with an organic binder (like plastic or wax). |
| 2. Injection Moulding | The mix is injected into a mould using a screw/barrel system like in plastic injection moulding. |
| 3. Binder Removal | The binder is removed by heating (thermal debinding) or with a solvent (chemical debinding). |
| 4. Sintering | The 'green' part (now binder-free) is sintered to achieve full density and strength. |

ADDITIVES

Additives are small amounts of extra substances added to ceramic powders to improve processing or final properties.

- Additive choice depends on:

  - Required green strength (how strong the part is before sintering).

  - Machinability – how easily it can be shaped.

  - Compatibility with the ceramic material.

  - The type of consolidation process (e.g., pressing, injection moulding).

- Organic additives like waxes, gums, thermoplastic resins:

  - Not water-soluble → not ideal for slip casting.

  - Good for injection moulding due to their meltability.

  - Can be burned off during sintering with minimal contamination.

- Inorganic binders remain part of the ceramic after processing.

Types of additives:

CERAMICS: STARTING POWDERS ARE DEPENDENT ON THE PROPERTIES REQUIRED IN THE FINISHED COMPONENT.

MUST BE PURE

MUST HAVE SMALL PARTICLES - SMALLER PARTICLES = MORE REACTIVE

Purity in Ceramics – Summary

- Purity greatly affects:

  - Mechanical strength

  - Stress rupture life

  - Oxidation resistance

- Impurity effects depend on:

  - The type of impurity

  - How it's distributed

  - Operating conditions (temperature, stress, time)

- Example:

  - Calcium (Ca) reduces creep resistance in Si₃N₄ when pressed with MgO.

  - But Ca has little effect when Y₂O₃ is used instead of MgO.

- For electrical, magnetic & optical ceramics:

  - Even tiny changes in impurity levels (DOPANT) can severely affect properties.

Particle Size and Reactivity – Summary

- Goal of consolidation: Maximize packing & uniformity → reduce shrinkage & porosity after sintering.

- Uniform size particles pack poorly → ~30% void space.

- Using mixed particle sizes (big + small + smaller) improves packing:

  - 2 sizes → voids ↓ to 26%

  - 3 sizes → voids ↓ to 23%

- Real ceramic particles are irregular → porosity often >50% before sintering.

- Low porosity & fine grains = high strength.

- For refractories (where strength isn't key), large particles or high porosity may be beneficial for:

  - Low thermal conductivity

  - High thermal shock resistance

Reactivity Slide:

- DENSIFICATION OF A COMPACTED POWDER AT HIGH TEMP is driven by  a change in surface free energy — particles bond to reduce this energy.

- Smaller particles (around 1 µm or less) have higher surface area thus high surface free energy therefore STRONGER THEMODYNAMIC DRIVE TO DECREASE THEIR AIREA BY BONDING TOGETHER. Making them more reactive and easier to bond and densify.

- For polycrystalline alumina for sodium vapour lamp envelopes to achieve transparent-  transparent ceramics (like in sodium lamp envelopes), pores bigger than 0.4 µm must be removed during sintering, as they scatter visible light and reduce transparency.

🟢 Small particles = more bonding
🔵 No big pores = better clarity

SINTERED SI3N4

- Larger particles (≈2 μm) → Only reach ~90% of theoretical density after sintering.

- Smaller particles (sub-micron) with high surface area (≥10 m²/g) → Achieve >95% density.

Why it matters:

Higher density means fewer pores, which leads to stronger, more reliable ceramics. So, using finer powders improves the quality of the final ceramic component.

POWDER SIZING

- Why size matters: Particle size and distribution affect the final properties (e.g. strength, density, wear resistance).

- Abrasives (wears down, smooth or clean surfaces eg sandpaper in ceramics - ALUMINA): These materials need to come in specific size ranges for effective use.

- Technique variety: Many powder synthesis and sizing methods exist to produce the exact particle size distributions needed for different applications.

👉 In short: Getting the right particle sizes is critical for the performance of ceramics, especially in abrasive or structural roles.

PARTICLE SIZE- Finer powders → better packing, sintering, and final ceramic properties like strength and density.

SINTERING

Sintering = Heating the compacted powder so particles bond and pores shrink or disappear, making the part denser and stronger.

To sinter, two things are needed:

- Transport mechanism – material must move from one particle to another.

- Energy source – usually heat, to drive that movement.

| Mechanism | Description |
| --- | --- |
| Vapour phase | Atoms move through gas/vapour between particles. |
| Solid state | Atoms move directly through solid contact (no melting). |
| Liquid phase | A small amount melts and helps other particles bond. |
| Reactive liquid | A liquid is formed during sintering via a chemical reaction, aiding bonding. |

| Process | Transport Mechanism | Driving Energy |
| --- | --- | --- |
| Vapour phase | Evaporation and condensation | Differences in vapour pressure |
| Solid state | Diffusion | Differences in free energy |
| Liquid phase | Viscous flow and diffusion | Capillary pressure, surface energy |
| Reactive liquid | Viscous flow + solution precipitation | Capillary pressure, surface energy |

VAPOUR PHASE SINTERING

“Movement from a positive radius of curvature to negative radius with a lower vapour pressure.”

- What it means: Atoms evaporate more easily from small curved surfaces (positive curvature) and move to areas with less curvature or indents (negative curvature).

- Why? Smaller particles have higher vapour pressure, so atoms “leave” more easily.

🔹 “Smaller particles therefore have a stronger driving pressure.”

- Smaller particles = higher surface energy = higher vapour pressure.

- So they evaporate more readily, driving material towards larger particles or neck regions.

🔹 “No shrinkage or densification.”

- Even though material is moving, the overall structure doesn’t compact or shrink.

- Only necks form between particles, but pores remain, so the part stays porous.

SOLID STATE SINTERING

- What happens?
Particles diffuse into each other through the solid phase (they stay solid the whole time).

- What drives it?
A drop in free energy (particles want to reduce their surface area, like a balloon deflating).

- Equation:
The equation just models how far particles "sink into" each other over time.

- This does cause densification—particles come closer together, pores shrink, structure gets stronger.

Reactivity in Ceramic Sintering – Summary

- Particle size and reactivity determine how quickly and at what temperature sintering happens.

- Smaller particles (finer powders) have more surface area, so they sinter faster and at lower temperatures.

- But: Long sintering times can cause grain growth, which reduces strength.

- So to keep ceramics strong, you want a powder that can densify quickly with minimal grain growth.